## Slide 1: Dating of artefacts using radioactive carbon 14C and determination of the elemental composition of pigments using the PIXE method
Karol Sučák, Miroslav Ješkovský , Boris Bobáľ, Jakub Kaizer, Ivan Kontuľ, Jakub Zeman, Pavel P. Povinec
Comenius University in Bratislava, Slovakia

## Slide 2: Paintings

## Slide 3: Paintings

## Slide 4: Paintings

## Slide 5: Paintings

## Slide 6: Methods
1.
2.
3.
Radiocarbon dating
PIXE method
Accelerator mass spectrometry (AMS) system diagram

## Slide 7: Methods
1.
2.
3.
Radiocarbon dating
PIXE method
Accelerator mass spectrometry (AMS) system diagram

## Slide 8: “Flowers and Fruits”
¹⁴C/¹²C
no Pb
Results from the radiocarbon age calibration of the painting, determined from the 14C / 12C ratio.
A piece of the wooden frame on which the canvas was stretched.

## Slide 9: “Flowers and Fruits”
¹⁴C/¹²C
no Pb
 | 1 | 2 | 3 | 4 | 5
Si | (62 ± 18)×103 | <5×103 | (22 ± 10)×103 | (76 ± 23)×103 | (55 ± 17)×103
S | (22 ± 2)×103 | (2.8 ± 0.6)×103 | (9 ± 1)×103 | (53 ± 6)×103 | (33 ± 3)×103
Cl | (3.8 ± 0.6)×103 | 740 ± 220 | <288 | (9 ± 2)×103 | (7.3 ± 0.9)×103
Ca | (70 ± 5)×103 | (36 ± 2)×103 | (15 ± 1)×103 | (37 ± 4)×103 | (16 ± 1)×103
Ti | (38 ± 3)×103 | (4.1 ± 0.4)×103 | (20 ± 1)×103 | (81 ± 8)×103 | (16 ± 1)×103
Fe | (6.9 ± 0.6)×103 | 530 ± 140 | (18 ± 1)×103 | (4.3 ± 0.6)×103 | (1.3 ± 0.2)×103
Zn | (100 ± 7)×103 | <127 | (21 ± 2)×103 | (68 ± 7)×103 | (217 ± 15)×103
Ba | (16 ± 4)×103 | (3 ± 1)×103 | (36 ± 4)×103 | (105 ± 13)×103 | (75 ± 6)×103
Measured element concentrations of “Flowers and fruits“ in ppm for individual colours.

## Slide 10: Conclusion
Radiocarbon dating (AMS) applied to determine painting age.
PIXE method identified several elements in different pigments.
These methods were also used for two more samples (more during poster session).

## Slide 11
THANK YOU FOR YOUR ATTENTION!
Acknowledgment:
This work was supported by Comenius University in Bratislava through the Young Researchers Grant (project UK/3172/2024) and by the Slovak Research and Development Agency (project APVV-21-0059).